TANKS

of

POLYESTER

REINFORCED WITH GLASS FIBER

CHEMICAL INDUSTRY, FOOD INDUSTRY, STORAGE OF FUELS, LIQUIDS AND SOLIDS IN GENERAL, DESALATION, DEPURATION EQUIPMENT

STANDARDS OF

PLACEMENT OF AERIAL HORIZONTAL TANKS

Tanks with cradle of G.R.P.

- BUPOLSA tanks must be installed on smooth, flat and uniform surfaces. With a rigid bed of sufficient resistance to pressure calculated by a competent technician

• Installation on flat and uniform surfaces:

The foundation must be flat and level with a difference of less than 2mm/m and a maximum total deviation of 5mm. The deposits must be placed or installed with a maximum deviation of 0.5º

• Installation using bed materials:

En caso de que la cimentación tenga desnivel o en caso de que las cunas de poliéster presenten huecos en la zona de apoyo se debe usar una masa niveladora (anticorrosiva si es preciso), de un espesor suficiente para asegurar el contacto entre la cimentación y las cunas. De esta manera todas las irregularidades, variaciones de uniformidad y pequeños defectos de las cunas, quedan totalmente cubiertos por esta masa expulsando el sobrante con el propio peso del depósito en el momento de su colocación.

If the foundation is uneven or if the polyester cradles have gaps in the support area, use a leveling compound (corrosion prevention if necessary) of sufficient thickness to ensure contact between the foundation and the cradles. In this way all the irregularities, variations of uniformity and small defects of the cradles, are totally covered by this mass expelling the surplus with the own weight of the deposit at the moment of its placement.

NOTE – The leveling mass, for example, cement mass, river sand, and mixtures of sand with bitumen, rubber, bituminous felt should be emplaced shortly before the erection, ensuring that the orientation marks are visible.

* IMPORTANT:

MAKE SURE OF THE CORRECT UNIFORMITY IN THE BANK, THE NON-EXISTENCE OF PUNZANT OBJECTS, PEBBLES, FRAGMENTS OF CONCRETE OR SOME TYPE OF STONE THAT CAN MARK AND DAMAGE THE CANS OF THE DEPOSIT.

IN THE SPREAD OF THE LEVELING MASS (ANTICORROSIVE IF IT IS NECESSARY) NEITHER MUST EXIST NO TYPE OF ROCK, STONES, PUNZANT OBJECTS ...

IN THE PLACEMENT OF THE TANK ON THE BASE, YOU MUST CHECK YOUR PERFECT SETTLEMENT AND THE UNEXISTENCE OF THE HOLLOWS BETWEEN THE BASE AND THE CRANES OF THE DEPOSIT.

IN THE POSITIONING OF THE BOLTS WHICH ARE LOCATED IN THE ANCHORS OF THE TANK, THE NUTS SHOULD BE TIGHTEN UNTIL IT COMES INTO ANCHORAGE AND NEVER THREW UP TO THE TOP, NEITHER LESS TO FORCE THE ANCHOR UNTIL THE BANK IS TOUCHED. ON THE BOTTOM, YOU MUST LEAVE THE CLEARANCE THAT REQUESTS THE TANK. (IN THE CASE OF CARRYING ANCHORS)

THE NON-COMPLIANCE OF THESE RECOMMENDATIONS CAN CAUSE, IN A FUTURE, THE RUPTURE OF THE FUND.

If something of the indicated in these instructions is not fulfilled the guarantee BUPOLSA would be invalidated